Gear Hobs & Shaper Cutters

Q: What gear accuracy grades can be achieved with JIAYI SEIKO’s gear hobs and shaper cutters?

A: Tool precision directly determines gear quality. JIAYI SEIKO's gear hobs are engineered and precision-ground to fully comply with DIN 3968 Class AA or Class A tolerances. For shaper cutters, we manufacture to DIN 1829 Class AA specifications. This micro-level tooth profile accuracy ensures that your finished gears easily hit strict AGMA or DIN quality standards, reducing post-heat treatment grinding times and minimizing gear running noise.

Q: What premium tool materials and coatings do you recommend for dry gear hobbing or cutting high-tensile alloy steels?

A: Gear cutting generates intense friction and heat, especially in modern dry-hobbing setups. To prevent rapid flank wear and cratering, JIAYI SEIKO utilizes premium powder metallurgy high-speed steel substrates (PM-HSS, such as S390 or ASP2060) which offer superior red hardness and toughness. We pair these with state-of-the-art Alcrona Pro or AlCrN nanocomposite coatings. These coatings exhibit an oxidation resistance temperature of up to 1, 100°C, significantly extending tool life and enabling higher cutting speeds ( VC ) in both wet and dry machining.

Q: When should I choose a multi-thread (multi-start) gear hob over a single-thread hob for production?

A: The choice is a balance between cycle time and surface quality:
1. Multi-Thread Hobs (2 to 4 starts): Drastically reduce roughing cycle times (e.g., a 2-start hob cuts machining time nearly in half), making them ideal for high-volume automotive gear roughing.
2. Single-Thread Hobs: Provide a higher number of generating cuts per tooth space, resulting in superior surface finish and a lower profile error. For high-precision finishing or heavy-module gears, single-thread tools remain the gold standard.

Q: Can JIAYI SEIKO design custom hobs and shaper cutters for special splines, non-involute profiles, or asymmetrical gear teeth?

A: Absolutely. Gear tooling profiles are highly specialized. Whether you need custom hobs for involute splines (DIN 5480, ANSI B92.1), parallel splines, sprocket teeth, worm gears, or complex non-standard asymmetrical tooth geometries for EV (Electric Vehicle) gearboxes, our engineering team can custom-design the precise tool profile. We use advanced gear simulation software to verify the generation process before manufacturing, guaranteeing a perfect tooth profile match. [Request a Custom Gear Tooling Blueprint & Quote].