Hole making tools

Q: What is the best tool sequence to achieve high-precision holes with tight cylindrical and surface finish tolerances?

A: To achieve micron-level tolerances (such as IT7 or higher) and an excellent surface finish (Ra< 0.8µm), a strategic multi-step or combined approach is required:
1. Pre-Drilling: Utilize JIAYI SEIKO's solid carbide drills (ideally with internal coolant) to create a straight, stable baseline hole.
2. High-Precision Reaming: Follow up with our custom carbide or cermet reamers. Reaming is critical for correcting cylindricity and achieving the final diameter with extreme accuracy.
3. Combined Options: For high-volume production, we engineer multi-step drills or composite drilling-reaming tools that combine multiple operations into a single pass, drastically reducing cycle times and eliminating tool-change errors.

Q: How can I prevent chip packing and tool breakage when drilling deep holes (5 x D to 30 x D‬‬)?

A: Deep hole drilling risks catastrophic failure if chips are not evacuated instantly. We recommend the following best practices:
1. Through-Coolant (Internal Coolant): Always use tools with internal coolant channels. High-pressure coolant forces chips back out along the flutes and cools the cutting zone directly.
2. Optimized Flute Geometry: JIAYI SEIKO's deep hole drills feature specialized wide-flute geometries and polished surfaces to minimize friction during chip transport.
3. Pecking Cycle: For extra-deep non-internal coolant setups, deploy a pecking cycle strategy to break and clear chips periodically, minimizing chip packing risks.

Q: When should I choose Cermet reamers over Carbide reamers for high-volume hole finishing?

A: Tool material selection depends heavily on your production volume and workpiece material:
1. Cermet Reamers: Best utilized for high-speed, high-volume finishing of steel, ductile iron, and automotive components. Cermet offers exceptional chemical stability and resistance to built-up edge (BUE), yielding a superior mirror-like surface finish and longer tool life under high-speed conditions.
2. Carbide Reamers: Ideal for a broader application spectrum, including stainless steel, titanium, and exotic alloys, due to its higher toughness and resistance to chipping under variable cutting conditions. [Inquire here to match the perfect tool material to your specific application].